Supplementary Information

Artificial neural network prediction of TiO2-doped chitosan micro/nanoparticle size based on particle imaging measurements

R. Seda TIĞLI AYDINa,*, Aysu DEMİRa

For Class 2 (TiO2-doped chitosan particle) simulation a total of 202 data (162 data for training and 40 data for testing) were used (Table 1).

Table 1. Training and test data set for TiO2-doped chitosan particles

| Mixing rate (rpm) | Chitosan:TPP (v/v) | Chitosan concentration (mg/ml) | TPP Concentration (mg/ml) | Particle Diameter (nm) |
| --- | --- | --- | --- | --- |
| 250 | 1.5 | 0.25 | 0.25 | 465.8776 |
| 250 | 1.5 | 0.25 | 0.5 | 511.9864 |
| 250 | 1.5 | 0.25 | 1 | 514.005 |
| 250 | 1.5 | 0.25 | 1.25 | 455.9382 |
| 250 | 1.5 | 0.25 | 2 | 482.2905 |
| 250 | 1.5 | 0.25 | 2.5 | 541.4143 |
| 250 | 1.5 | 0.25 | 3 | 490.1887 |
| 250 | 1.5 | 0.25 | 3.5 | 531.4709 |
| 250 | 1.5 | 0.25 | 4 | 449.4858 |
| 250 | 1.5 | 0.25 | 5 | 454.6764 |
| 250 | 1.5 | 0.25 | 0.75 | 517.142 |
| 250 | 1.5 | 0.5 | 0.25 | 512.6078 |
| 250 | 1.5 | 0.5 | 0.5 | 427.3397 |
| 250 | 1.5 | 0.5 | 0.75 | 457.4509 |
| 250 | 1.5 | 0.5 | 1 | 482.9453 |
| 250 | 1.5 | 0.5 | 1.5 | 454.0678 |
| 250 | 1.5 | 0.5 | 2 | 493.0745 |
| 250 | 1.5 | 0.5 | 3.5 | 490.8668 |
| 250 | 1.5 | 0.5 | 4 | 508.1655 |
| 250 | 1.5 | 0.5 | 4.5 | 594.1737 |
| 250 | 1.5 | 0.75 | 0.25 | 492.485 |
| 250 | 1.5 | 0.75 | 0.5 | 641.0112 |
| 250 | 1.5 | 0.75 | 0.75 | 502.6796 |
| 250 | 1.5 | 0.75 | 1 | 495.5587 |
| 250 | 1.5 | 0.75 | 2 | 534.9981 |
| 250 | 1.5 | 0.75 | 2.5 | 470.2394 |
| 250 | 1.5 | 0.75 | 3 | 484.786 |
| 250 | 1.5 | 0.75 | 3.5 | 619.6193 |
| 250 | 1.5 | 0.75 | 4 | 442.1088 |
| 250 | 1.5 | 0.75 | 4.5 | 484.8413 |
| 250 | 1.5 | 0.75 | 5 | 487.395 |
| 250 | 1.5 | 1 | 0.25 | 500.3393 |
| 250 | 1.5 | 1 | 0.5 | 608.4317 |
| 250 | 1.5 | 1 | 0.75 | 468.3143 |
| 250 | 1.5 | 1 | 1.25 | 533.1934 |
| 250 | 1.5 | 1 | 1.5 | 487.5921 |
| 250 | 1.5 | 1 | 2.5 | 492.1481 |
| 250 | 1.5 | 1 | 3.5 | 478.5891 |
| 250 | 1.5 | 1 | 4 | 472.1529 |
| 250 | 1.5 | 1 | 5 | 510.1773 |
| 250 | 1 | 1.5 | 0.25 | 528.3867 |
| 250 | 2 | 1 | 1 | 526.5358 |
| 250 | 2 | 2.5 | 0.5 | 506.4315 |
| 500 | 2 | 0.25 | 0.25 | 647.7425 |
| 500 | 1.5 | 0.25 | 0.25 | 588.1474 |
| 500 | 1.5 | 0.25 | 0.5 | 594.8303 |
| 500 | 1.5 | 0.25 | 0.75 | 599.117 |
| 500 | 1.5 | 0.25 | 1 | 596.9388 |
| 500 | 1.5 | 0.25 | 1.25 | 607.9808 |
| 500 | 1.5 | 0.25 | 1.5 | 601.5576 |
| 500 | 1.5 | 0.25 | 2 | 579.4551 |
| 500 | 1.5 | 0.25 | 2.5 | 612.6943 |
| 500 | 1.5 | 0.25 | 3 | 588.7582 |
| 500 | 1.5 | 0.25 | 3.5 | 587.9739 |
| 500 | 1.5 | 0.25 | 4 | 579.253 |
| 500 | 1.5 | 0.25 | 4.5 | 582.1327 |
| 500 | 1.5 | 0.5 | 0.25 | 651.5528 |
| 500 | 1.5 | 0.5 | 0.5 | 607.5628 |
| 500 | 1.5 | 0.5 | 0.75 | 640.9233 |
| 500 | 1.5 | 0.5 | 1 | 623.1681 |
| 500 | 1.5 | 0.5 | 1.25 | 610.1126 |
| 500 | 1.5 | 0.5 | 2 | 607.1735 |
| 500 | 1.5 | 0.5 | 3 | 600.7028 |
| 500 | 1.5 | 0.5 | 3.5 | 603.4766 |
| 500 | 1.5 | 0.5 | 4 | 594.867 |
| 500 | 1.5 | 0.5 | 4.5 | 605.6449 |
| 500 | 1.5 | 0.5 | 5 | 572.2162 |
| 500 | 1.5 | 0.75 | 0.25 | 697.9443 |
| 500 | 1.5 | 0.75 | 0.5 | 591.3738 |
| 500 | 1.5 | 0.75 | 0.75 | 584.4912 |
| 500 | 1.5 | 0.75 | 1 | 583.0796 |
| 500 | 1.5 | 0.75 | 1.25 | 577.3817 |
| 500 | 1.5 | 0.75 | 2 | 583.7645 |
| 500 | 1.5 | 0.75 | 2.5 | 575.1604 |
| 500 | 1.5 | 0.75 | 3.5 | 553.2687 |
| 500 | 1.5 | 0.75 | 4 | 608.9508 |
| 500 | 1.5 | 0.75 | 4.5 | 581.471 |
| 500 | 1.5 | 0.75 | 5 | 552.7175 |
| 500 | 1.5 | 1 | 0.25 | 583.7738 |
| 500 | 1.5 | 1 | 0.5 | 715.1129 |
| 500 | 1.5 | 1 | 0.75 | 616.6498 |
| 500 | 1.5 | 1 | 1 | 612.7607 |
| 500 | 1.5 | 1 | 1.5 | 624.0728 |
| 500 | 1.5 | 1 | 2 | 784.917 |
| 500 | 1.5 | 1 | 2.5 | 615.7925 |
| 500 | 1.5 | 1 | 3 | 633.4636 |
| 500 | 1.5 | 1 | 3.5 | 604.5038 |
| 500 | 1.5 | 1 | 4 | 562.5384 |
| 500 | 1.5 | 1 | 4.5 | 641.1632 |
| 500 | 1.5 | 1 | 5 | 608.2476 |
| 500 | 1.5 | 1.25 | 0.25 | 527.7788 |
| 500 | 1.5 | 1.25 | 1.5 | 584.2413 |
| 500 | 1.5 | 1.5 | 0.25 | 590.2953 |
| 500 | 1.5 | 2 | 1.5 | 596.7241 |
| 500 | 1.5 | 2 | 4.5 | 564.1721 |
| 500 | 1.5 | 2 | 5 | 613.2318 |
| 500 | 1.5 | 2.5 | 0.25 | 698.7009 |
| 500 | 1.5 | 2.5 | 0.75 | 599.2316 |
| 500 | 1.5 | 2.5 | 4 | 585.5054 |
| 500 | 1.5 | 2.5 | 4.5 | 582.463 |
| 500 | 1.5 | 2.5 | 5 | 565.4632 |
| 500 | 1.5 | 3 | 0.75 | 606.5913 |
| 500 | 1.5 | 3 | 1 | 546.5014 |
| 500 | 1.5 | 3 | 3.5 | 571.6494 |
| 500 | 1.5 | 3.5 | 1 | 604.5086 |
| 500 | 1.5 | 3.5 | 3 | 611.0133 |
| 500 | 1.5 | 3.5 | 4 | 630.6159 |
| 500 | 1.5 | 3.5 | 5 | 751.7468 |
| 500 | 1.5 | 4 | 0.75 | 569.2601 |
| 500 | 1.5 | 4.5 | 1.5 | 600.2451 |
| 750 | 1 | 0.25 | 0.25 | 673.3683 |
| 750 | 1 | 0.25 | 0.5 | 691.6549 |
| 750 | 1 | 0.25 | 0.75 | 637.7152 |
| 750 | 1 | 0.25 | 1 | 660.9224 |
| 750 | 1 | 0.25 | 1.25 | 672.9142 |
| 750 | 1 | 0.25 | 1.5 | 646.6116 |
| 750 | 1 | 0.25 | 2 | 691.3456 |
| 750 | 1 | 0.25 | 2.5 | 672.8859 |
| 750 | 1 | 0.25 | 3 | 655.9974 |
| 750 | 1 | 0.25 | 3.5 | 675.6498 |
| 750 | 1 | 0.25 | 4 | 674.7711 |
| 750 | 1 | 0.25 | 4.5 | 653.2562 |
| 750 | 1 | 0.25 | 5 | 663.3117 |
| 750 | 1 | 0.5 | 0.25 | 633.5456 |
| 750 | 1 | 0.5 | 0.5 | 742.6152 |
| 750 | 1 | 0.5 | 0.75 | 647.1168 |
| 750 | 1 | 0.5 | 1 | 656.4604 |
| 750 | 1 | 0.5 | 1.25 | 654.5659 |
| 750 | 1 | 0.5 | 1.5 | 623.2229 |
| 750 | 1 | 0.5 | 2 | 689.0514 |
| 750 | 1 | 0.5 | 2.5 | 717.4743 |
| 750 | 1 | 0.5 | 3 | 660.2039 |
| 750 | 1 | 0.5 | 3.5 | 639.959 |
| 750 | 1 | 0.5 | 4 | 644.8603 |
| 750 | 1 | 0.5 | 4.5 | 649.2255 |
| 750 | 1 | 0.5 | 5 | 650.1691 |
| 750 | 1 | 0.75 | 0.25 | 632.8059 |
| 750 | 1 | 0.75 | 0.5 | 634.512 |
| 750 | 1 | 0.75 | 0.75 | 673.2337 |
| 750 | 1 | 0.75 | 1 | 639.7098 |
| 750 | 1 | 0.75 | 1.25 | 622.6948 |
| 750 | 1 | 0.75 | 1.5 | 627.7486 |
| 750 | 1 | 0.75 | 2 | 632.1257 |
| 750 | 1 | 0.75 | 2.5 | 635.1261 |
| 750 | 1 | 0.75 | 3 | 686.3247 |
| 750 | 1 | 0.75 | 3.5 | 756.3518 |
| 750 | 1 | 0.75 | 4 | 648.6605 |
| 750 | 1 | 0.75 | 4.5 | 798.4032 |
| 750 | 1 | 0.75 | 5 | 627.1367 |
| 750 | 1 | 1 | 0.25 | 638.3086 |
| 750 | 1 | 1 | 0.5 | 670.3881 |
| 750 | 1 | 1 | 0.75 | 734.6227 |
| 750 | 1 | 1 | 1 | 641.9584 |
| 750 | 1 | 1 | 1.25 | 628.1025 |
| 750 | 1 | 1 | 1.5 | 708.6779 |
| 750 | 1 | 1 | 2 | 1018.878 |
| 750 | 1 | 1 | 2.5 | 628.5768 |
| 750 | 1 | 1 | 3 | 681.8713 |
| 750 | 1 | 1 | 3.5 | 669.3524 |
| 750 | 1 | 1 | 4 | 630.1708 |
| 750 | 1 | 1 | 4.5 | 637.8134 |
| 750 | 1 | 1 | 5 | 650.5883 |
| 750 | 1 | 1.25 | 0.25 | 1137.263 |
| 750 | 1 | 1.25 | 0.5 | 1095.963 |
| 750 | 1 | 1.25 | 0.75 | 916.4135 |
| 750 | 1 | 1.25 | 1 | 849.5306 |
| 750 | 1 | 1.25 | 1.25 | 713.5792 |
| 750 | 1 | 1.25 | 1.5 | 669.7996 |
| 750 | 1 | 1.25 | 2 | 602.0655 |
| 750 | 1 | 1.25 | 2.5 | 670.9604 |
| 750 | 1 | 1.25 | 3 | 701.4699 |
| 750 | 1 | 1.25 | 3.5 | 681.1113 |
| 750 | 1 | 1.25 | 4 | 621.0949 |
| 750 | 1 | 1.25 | 4.5 | 643.1199 |
| 750 | 1 | 1.25 | 5 | 639.1918 |
| 750 | 1 | 1.5 | 0.25 | 658.4007 |
| 750 | 1 | 1.5 | 0.5 | 669.5444 |
| 750 | 1 | 1.5 | 0.75 | 623.2249 |
| 750 | 1 | 1.5 | 1 | 694.1076 |
| 750 | 1 | 1.5 | 1.25 | 679.2576 |
| 750 | 1 | 1.5 | 1.5 | 701.8077 |
| 750 | 1 | 1.5 | 2 | 631.1938 |
| 750 | 1 | 1.5 | 2.5 | 698.2861 |
| 750 | 1 | 1.5 | 3 | 657.5077 |
| 750 | 1 | 1.5 | 3.5 | 687.5417 |
| 750 | 1 | 1.5 | 4 | 655.2583 |
| 750 | 1 | 1.5 | 4.5 | 657.3452 |
| 750 | 1 | 1.5 | 5 | 670.1132 |
| 750 | 1 | 2 | 0.25 | 656.4912 |
| 750 | 1 | 2 | 0.5 | 655.5702 |
| 750 | 1 | 2 | 0.75 | 605.9435 |
| 750 | 1 | 2 | 1 | 612.2258 |
| 750 | 1 | 2 | 1.25 | 770.7549 |
| 750 | 1 | 2 | 1.5 | 645.642 |
| 750 | 1 | 2 | 2 | 648.093 |
| 750 | 1 | 2 | 2.5 | 675.1885 |
| 750 | 1 | 2 | 3 | 668.1128 |
| 750 | 1 | 2 | 3.5 | 673.5869 |
| 750 | 1 | 2 | 4 | 628.3611 |
| 750 | 1 | 2 | 4.5 | 622.7945 |
| 750 | 1 | 2 | 5 | 645.6064 |
| 750 | 1 | 5 | 4 | 628.4261 |